## Slide 1
Alaska Department of Transportation & Public Facilities
Anchorage International’s
First Concrete Runway
Three Years In
Mitch Miller, PE
ADOT&PF Central Region Materials
November 24th, 2014

## Slide 2: ANC Background
Alaska’s Largest Airport
Three runways over 10,600 ft.
    One over 12,000 ft
Equidistant from Tokyo and New York
The primary stopover for cargo moving between the US and Asia
  9 hours from 90% of the industrialized world

## Slide 3: ANC Background

## Slide 4
2013 WORLDS TOP 10 BUSIEST CARGO AIRPORTS |  | 
RANK | AIRPORT | 1,000's tons
1st | Memphis | 4,134
2nd | Hong Kong | 4,127
3rd | Shanghai Pudong International | 2,856
4th | Dubai International | 2,436
5th | Anchorage International (ANC) | 2,421
6th | Seoul Incheon International | 2,395
7th | Louisville International | 2,145
8th | Fankfurt International | 2,016
9th | Tokyo Narita International | 1,980
10th | Miami International | 1,909
Notes: 5th busiest in the world
AND
2nd busiest in the US

## Slide 5: ANC Background
ANC’s Three Runways
  N-S Runway 14-32
  E-W Runways 7R-25L and 7L-25R
  All Asphalt Pavements Historically

## Slide 6: Project Background
  Runway 7R-25L
    Originally constructed in 1969
      4” HMA over
        8” Bituminous Base Course
        100+” Subbbase
    Supports the majority of “Wide Body” Traffic (B-747, B-777, A-340, MD 11, etc.)
    Intermittent shave and pave rehabs
    After increasing frequency of partial rehabs full reconstruction was in order

## Slide 7: ANC Background

## Slide 8: Project Background
  2010 - Phase I of the reconstruction project rehabilitated the east half of 7R with HMA surface
  2011 - Phase II reconstructed and extended the west half of the runway including 5,000 ft PCC concrete keel

## Slide 9: Project Background
  PCC section was located at the west end of the runway in the touchdown area of 7R
      Where the asphalt runway repairs were most often required
  PCC pavement designed using FAA AC 150/5320-6E Airport Pavement Design and Evaluation
Notes: Where the historical damage has occurred requiring shave and pave rehabs the most frequently

## Slide 10: Project Background
  Resulting PCC Pavement Design
  21” PCC slab depth (26” at edge)
        Included 4” stabilized base
        95” Subbase
  PCC Keel varied in width from 100 ft to 80 ft
  Approx. 20’x20’ slab dimension
  1.5” x 24” dowel bars 12” OC spacing through all joints

## Slide 11: Project Background
  Contract Requirements for PCC Pavement Construction
  A PCC super intendant with min. 10 years experience on similar scale projects
  Required slip form placement of PCC

## Slide 12: Project Background

## Slide 13: Project Background

## Slide 14: Project Background

## Slide 15: Project Background

## Slide 16: Project Background

## Slide 17: Project Background

## Slide 18: Project Background

## Slide 19
Project Background
Construction went smoothly (relatively) until…
Notes: Relatively

## Slide 20: 7R-25L Canal
Project Background

## Slide 21: Project Background

## Slide 22: Project Background
  Original Construction Summary
  Some uncontrolled cracking resulted in a few slab replacements and some minor cracks being filled with epoxy resin

## Slide 23: Project Background
  Issues following first winter in service
  Record snowfall 2011-2012 (133 inches at ANC)
  Edge spalling created FOD on the runway (particularly at centerline)
  Preformed compression seals depressed into joint reservoir
  1”-3” Heave between HMA and PCC

## Slide 24: Partial Depth Repair (PDR)
  Summer 2014 the Department completed a mock up PDR project to test repair practices in anticipation of a larger PDR project in the coming years.
  The initial project determined:
  how deep a typical repair will be (needed to define scope for bidding)
  a baseline tensile strength of the existing concrete so an acceptance bond strength can be set
  removal and prep practices that provided the best bond between patch material and existing concrete
  Concrete Consulting Engineers, LLC (CCE) helped the Department put the project together and is helping with the distillation of collected information.
Notes:   Its purpose was to define an effective procedure for edge spall repair and determine an acceptance criteria on which future work can be accepted.

## Slide 25: Partial Depth Repair (PDR)
  Mock up description:
  Twenty five (25) 20’x20’ panels were selected for PDR work
  Approximately 40 repairs were performed on those 25 panels
  The entire centerline along the test site was removed and replaced
  Repair materials included standard concrete, elastomeric concrete and FAA approved epoxy resin
  Tensile strength of existing concrete and bond between the patch and existing concrete was tested using ASTM C1583
  Remove and replace existing preformed compression seal with a wider version to increase sidewall pressure
  Note: ASTM C 1583 Standard Test Method for Tensile Strength of Concrete Surfaces and the Bond Strength or Tensile Strength of Concrete Repair and Overlay Materials by Direct Tension

## Slide 26: Partial Depth Repair (PDR)
  ASTM C 1583 Test Device

## Slide 27: Partial Depth Repair (PDR)

## Slide 28: Partial Depth Repair (PDR)
  REMOVAL: Multiple methods were used
  Chipping hammer (15-lb max)
  Mill
  Hydrodemolition
  Tensile strength testing of the prepped surface was performed to determine which method produced the least amount of substrate bruising.
  Testing in cavities was challenging.

## Slide 29: Partial Depth Repair (PDR)

## Slide 30: Partial Depth Repair (PDR)

## Slide 31: Partial Depth Repair (PDR)

## Slide 32: Partial Depth Repair (PDR)

## Slide 33: Partial Depth Repair (PDR)

## Slide 34: Partial Depth Repair (PDR)
  Testing Bond Between Patch Material and Substrate
  ASTM C 1583 used again to test the bond strength of the patch material to the existing concrete. The expectation is the result should be at least as high as the tensile strength of the substrate PCC.

## Slide 35: Partial Depth Repair (PDR)

## Slide 36: Partial Depth Repair (PDR)

## Slide 37: Partial Depth Repair (PDR)
  Results
  Looks like hydrodemolition is the way to go for removal
  Repair depths will be approximately 3-4 inches deep
  Repair materials will be monitored for performance over the winter
  PCC is the easiest material to place
  Repair areas were wider for mock up project so we could test substrate at each location
  We will probably not fix as many spalls as originally planned
    (probably use a liquid sealant along joint faces where multiple small spalls have resulted in a rough reservoir edge)

## Slide 38: Maintenance
  Observed differences between
  PCC vs. HMA
  PCC requires extra chemical treatment (often prior to anticipated snow or ice events) due to increased icing and reluctance to use hard edged removal equipment
  PCC repairs take more thought, time and expertise to perform properly
  Considerable heaving issues the first winter along the HMA-PCC longitudinal joint (less of problem the following winter)

## Slide 39: Future PCC Pavements
  Large busy taxiway intersection that supports a lot of “wide body” turning movements.

## Slide 40: Future PCC Pavements
    Questions?